Introduction to Semiconductor Devices

(Purdue University EE 305)

Supplemental Homework Exercises

Tutorial question based on crystals using the crystal viewer program on http://nanoHUB.org.

Reference / course book: Semiconductor Device Fundamentals by Robert E. Pierret

Q1. Exercise 1.1 from the book.

Q2. What are the various Bravais lattices ?

Q3. How many atoms per unit cell are present in the following Bravais lattices :

[a] Face Centered Cubic

[b] Body Centered Orthorhombic.

[c] Hexagonal

Q4. What are the crystal systems for the following materials:

[1] Silicon

[2] Gallium Arsenide (GaAs).

Q5. Exercise 1.2 from the book.

Q6. Draw the miller planes for the following miller indices and verify using the crystal viewer program:

[a] 2 0 0   [b] 3 2 1  [c] 0 2 4   [d] 2 3 6

Q7. Exercise 1.4(b). Verify the result using crystal viewer program.